深 圳 市 优 三 科 技 有 限 公 司

Shenzhen You-San Technology Co.,Ltd

编制日期：2022/10/14           版本：A/0

产品技术说明书

Product technical specification

- 产品描述 Product Description

高性能无基材双面胶带是在离型纸上均匀涂高性能丙烯酸酯压敏胶制作而成。其具有优良的粘合效果、耐候性佳、良好的耐温性、耐水性佳、能防止脱落与变形等状况发生，并且易于冲型模切。

High performance non substrate double-sided tape is made by evenly coating high-performance acrylic pressure sensitive adhesive on release paper. It has excellent bonding effect, good weather resistance, good temperature resistance, good water resistance, can prevent detachment and deformation, and is easy to punch and die cut.

- 产品结构 Product structure

丙烯酸酯胶

离型纸

- 主要用途 Main Use

- 薄膜开关：含柔性、硬性、凹凸等类别的薄膜开关。

Membrane switch: including flexible, rigid, concave and convex Membrane switch.

- 铭牌、标志：应用在丝网印刷、广告、航空、医疗及工业设备、汽车、家电、电子市场等行业上。

Nameplates and logos: Used in industries such as screen printing, advertising, aviation, medical and industrial equipment, automobiles, home appliances, and electronic markets.

- 显示屏以及面板：应用在3C数码，家用电器以及智能家居行业上。

Display screen and panel: 3C digital, household appliances, and smart home industry

- FPC软板：应用在手机、笔记本电脑、PDA、数码相机、LCM等电子产品上。

Softboard FPC: Used in electronic products such as mobile phones, laptops, PDAs, digital cameras, LCMs, etc.

- 防震泡棉：泡棉背胶，防震固定。

Shockproof foam: Foam back adhesive, shockproof and fixed.

- 无纺布粘贴：用于医疗行业无纺布粘接固定。

Non woven fabric bonding: used for bonding and fixing non-woven fabrics in the medical industry.

- 金属板类粘贴：用于各类金属板、塑料板和纸盒类材料的粘贴。

Metal plate pasting: used for pasting various metal plates, plastic plates, and paper box materials.

- 产品特性 Product Features

- 优良的粘合效果

Excellent bonding effect

- 有较强的抗静态应力和动态应力，可抵抗一定的震动冲击

Strong resistance to static and dynamic stresses, capable of withstanding certain vibrations and impacts

- 良好的耐温性

Good temperature resistance

- 耐候性佳

excellent weatherability

- 易冲型模切

Easy punching die cutting

- 典型性能 Typical performance

| 项 目Test items | 测试方式Test method | 单位Unit | P3310A |
| --- | --- | --- | --- |
| 颜色Color | 目测Visual inspection | - | 透明transparent |
| 胶系Type of glue | - | - | 丙烯酸酯Acrylate adhesive |
| 离型材料Release material | - | - | 离型纸Release paper |
| 总厚度Total thickness | ASTM D-3652 | mm | 0.1 |
| 180°剥离强度（钢板，20min）180°Peel strength（SUS，20min） | GB/T2792-2014 | N/inch | 16 |
| 常温保持力Room temperature retention | GB/T4851-2014 | min（25℃，1000g） | ≥10000 |
| 环形初粘力（Annular initial adhesion force） | GB/T 31125-2014 | N/inch | 14 |
| 长期耐温性Long term temperature resistance | GB∕T 4851-2014 | ℃ | 80 |
| 短期耐温性Short term temperature resistance | GB∕T 4851-2014 | ℃ | 120 |

- 产品规格 Product specifications

- 1240mm*55m

- 或其他定制

Other customization

- 储存及保质期 Storage and shelf life

建议存放在清洁干燥的地方，防止包装破损，避免与挥发性溶剂放在一起。存储温度为4～26℃，湿度为40～50%。

It is recommended to store them in a clean and dry place to prevent package damage and volatile solvents. The storage temperature is 4~26 ℃, and the humidity is 40~50%.

为保持最佳性能，本品应在生产之日起6个月内使用。

To maintain the best performance, this product should be used within 6months from the date of production.

- 声明 Statement

上述测试结果仅为典型值，并非保证值。如果有新的认识和新的经验出现，优三会相应修改此资料，且不再另行通知。优三强烈推荐客户在使用产品前进行独立的测试，以了解产品的适用性。

The above test results are only typical values, not guaranteed values. In case of new knowledge and experience, Yousan will modify this information accordingly without further notice. Yousan strongly recommends that customers conduct independent tests before using the product to understand the applicability of the product.